Received: 24 April 2024 | Revised: 21 June 2024 | Accepted: 24 July 2024	 DOI: 10.1002/ese3.1861

CHALLE NGES TO INDUSTR Y

A review of challenges with using the natural gas system for hydrogen

## Paul Martin1	|	Ilissa B. Ocko2,3 	|	Sofia Esquivel‐Elizondo4 	|

Roland Kupers5	|	David Cebon6	|	Tom Baxter7	|	Steven P. Hamburg2

Abstract

Hydrogen, as an energy carrier, is attractive to many stakeholders based on the assumption that the extensive global network of natural gas infrastructure can be repurposed to transport hydrogen as part of a zero‐carbon energy future. Therefore, utility companies and governments are rapidly advancing efforts to pilot blending low‐carbon hydrogen into existing natural gas systems, many with the goal of eventually shifting to pure hydrogen. However, hydrogen has fundamentally different physical and chemical properties to natural gas, with major consequences for safety, energy supply, climate, and cost. We evaluate the suitability of using existing natural gas infrastructure for distribution of hydrogen. We summarize differences between hydrogen and natural gas, assess the latest science and engineering of each component of the natural gas value chain for hydrogen distribution, and discuss proposed solutions for building an effective hydrogen value chain. We find that every value chain component is challenged by reuse. Hydrogen blending can circumvent many challenges but offers only a small reduction in greenhouse gas emissions due to hydrogen's low volumetric energy density. Furthermore, a transition to pure hydrogen is not possible without significant retrofits and replacements. Even if technical and economic barriers are overcome, serious safety and environ- mental risks remain.

KE YW OR DS

alternative fuels, decarbonization, energy, hydrogen, natural gas

1Spitfire Research Inc., Toronto, Ontario, Canada

2Environmental Defense Fund, New York, New York, USA

3Now at U.S. Department of State, Washington, District of Columbia, USA

4Environmental Defense Fund Europe, Amsterdam, The Netherlands

5Thunderbird School of Global Management, University of Arizona, Tucson, Arizona, USA

6Engineering Department, Cambridge University, Cambridge, UK

7Department of Chemical Engineering, University of Strathclyde, Glasgow, UK

Correspondence

Steven P. Hamburg, Environmental Defense Fund, 257 Park Ave S, New York, NY 10010, USA.

Email: shamburg@edf.org

# |	INTRODUCTION

Natural gas is an integral component of the world's current energy system, accounting for around a quarter of today's final energy demand globally.1 Natural gas is principally comprised of methane (CH4), with smaller amounts of mostly ethane and carbon dioxide (CO2)—all

of fossil origin. Natural gas combustion is estimated to account for around 30% of annual global anthropogenic CO2 emissions.2 Furthermore, a growing body of research has revealed the extent of gas lost to the atmo- sphere throughout the supply chain, which is estimated to account for 12% of annual global anthropogenic methane emissions.3 Together, CO2 and CH4 are

This is an open access article under the terms of the Creative Commons Attribution License, which permits use, distribution and reproduction in any medium, provided the original work is properly cited.

© 2024 The Author(s). Energy Science & Engineering published by Society of Chemical Industry and John Wiley & Sons Ltd.

Energy Sci. Eng. 2024;12:3995–4009.	wileyonlinelibrary.com/journal/ese3	|	3995

MARTIN ET AL.

3996	|

responsible for around 75% of today's gross warming relative to the beginning of the industrial revolution.4 Whereas experts suggest that we have the technologies available to cut CH4 emissions from oil and gas opera- tions by 75%,3 a transition away from fossil fuels and their combustion, including natural gas, is needed to achieve climate goals.5 Therefore, an obvious way to maintain beneficial use of the extensive and valuable global network of natural gas infrastructure during the impending energy transition would require switching to a gas/gas mixture that does not generate greenhouse gas (GHG) emissions when combusted.

Hydrogen (H2) has emerged as a natural gas replacement, because it can release energy without associated carbon dioxide emissions. The chemical en- ergy stored in the hydrogen to hydrogen bond can be converted to either heat through combustion or elec- tricity in a fuel cell with no CO2 emissions: processes that humans have been employing for more than 100 years.6 H2 cannot currently be considered an energy source like natural gas, because it is being produced through meth- ods such as electrolysis or steam reforming.7 There are numerous techniques available to manufacture hydrogen from feedstock molecules, including natural gas but also water. Currently, 99% of dedicated H2 production relies on fossil fuels without carbon capture,3 emitting over 900 million metric tonnes of CO2 into the atmosphere annually.3 There are more than a 1000 proposed projects aimed at scaling up zero‐ and low‐carbon hydrogen production processes globally.8 There are challenges associated with each “clean” hydrogen production method as well—and no method is universally beneficial to the climate.9–12 For example, renewable energy dis- placement or high methane emissions can make hydro- gen applications worse for the climate in the near‐term than the fossil fuel systems they are replacing.13

Although reusing natural gas infrastructure for hydrogen is an appealing proposition, its feasibility rests on the suitability of the existing gas network for hydro- gen gas. Decades ago, gas mixtures made by gasification of either coal or petroleum—known as “town gas”— contained high concentrations (up to 50% by volume) of H2,14 and were piped into homes. Therefore, the distri- bution infrastructure could technically tolerate high levels of hydrogen. Although gas produced by gasifica- tion of petroleum naphtha and natural gas is still used in locations like Singapore and Hong Kong, this method has been abandoned in most of the world for safer options (natural gas), which do not contain toxic carbon mon- oxide. Therefore, most gas networks today are almost entirely designed for fossil gas mixtures that are pri- marily comprising methane (75% to 90%+ by volume, containing very little if any H2). Material selection,

system attributes, storage systems, appliances and device design, and so on were designed, tested, and optimized specifically for the characteristics of natural gas and not for those of H2. The fundamental differences in physical and chemical properties of H2 and CH4 are quite large, leading to challenges with respect to safety, energy sup- ply, climate impacts, and cost.

In the following sections, we address the practicality, risks, and remaining data gaps of using H2 in existing natural gas infrastructure by (1) contrasting physical and chemical properties between H2 and CH4; (2) describing how these differences affect each component of the ex- isting natural gas system value chain; (3) discussing potential strategies to mitigate issues; and (4) the chal- lenges associated with implementing such solutions.

# |	CONSTRASTING PROPERTIES OF HYDROGEN AND

NATURAL GAS

Although both colorless and odorless gases at standard temperature and pressure, H2 and CH4 are very different gases both physically and chemically (see Table 1). These differences present many challenges when considering the use of natural gas infrastructure for H2, which are further discussed in Section 3. In addition, while CH4 in the atmosphere absorbs radiation whereas H2 does not, both can be oxidized leading to perturbations to atmospheric chemistry in ways that lead to increases in other GHGs.

## |	Physical

There are two key physical differences between H2 and CH4 that relate to their molecular sizes and liquid phase temperatures. First, hydrogen is the smallest and lightest element on the periodic table. A molecule of hydrogen— consisting of two hydrogen atoms—is therefore the smallest and lightest molecule. H2's weight and density is one‐eighth that of CH4 and its diffusivity in air is around three times higher (see Table 1). This means that H2 can more rapidly leak from infrastructure, permeate through materials, and rise and accumulate at high points in enclosed spaces.15

Second, the temperatures at which H2 and CH4 can be converted into a liquid, which can be useful as a storage and transport mechanism, are −253°C and

−162°C at atmospheric pressure, respectively. Thus, much more energy is needed to convert H2 gas into a liquid and it is more likely to incur H2 losses through evaporation given the high temperature difference between the liquid and the surrounding environment.

|

3997

MARTIN ET AL.

TABLE 1  Characteristics of hydrogen compared to natural gas (methane) and their implications.

|  | Property | Hydrogen (H2) | Methane (CH4) | Hydrogen compared to natural gas (mostly CH4) | Implications of H2 compared to natural gas |
| --- | --- | --- | --- | --- | --- |
| Physical |  |  |  |  |  |
| Size | Molecular weight, g/mol | 2.106 | 16.04 | ~8× lighter | Permeates faster from gaskets, seals, plastic pipes, and other “soft” materials |
| Density | Density (NTP), kg/m3 | 0.08375 | 0.668 | ~8× lower density | Rises and accumulates in enclosed spaces |
| Diffusion | Diffusion coefficient in air, m2/s (20°C) | 7.56E−05 | 2.21E−05 | Higher diffusivity | Overall tendency to leak at a greater extent through intact materials of construction, seals, and piping joints |
|  | Diffusion coefficient in water, m2/s (20°C) | 4.58E−09 | 1.62E−09 |  |  |
| Liquid phase | Temperature at atmospheric pressure (°C) | −253 | −162 | ~100°C colder | Requires much more energy to convert to liquid state; more rapid boil‐off |
| Chemical |  |  |  |  |  |
| Chemistry | Reactivity | H‐H bond | C‐H bond | Formation of partial bonds which | Accelerates fatigue cracking and reduces fracture |
|  |  | symmetry | asymmetry | lower activation energy | toughness of steels |
|  |  |  |  |  | May be depleted in underground storage |
| Ignition | Explosive limits, % ‐ %, by | 4–75 | 5.3–15 | Higher explosive limit | Higher fire risk |
|  | volume |  |  |  |  |
|  | Ignition energy mJ | 20 | 290 | Lower ignition energy |  |
| Flame | Maximum flame speed, m/s | 0.34 | 2.9 | ~8× faster flame speed | Lower flame stability in burners, risk of flash‐back |
|  | Flame color | Invisible in | Blue | Lower visibility | Harder to detect |
|  |  | daylight |  |  |  |
|  | Adiabatic flame temperature | 2210 | 1950 | Higher temperature | More NOx produced |
|  | in air,°C |  |  |  |  |
| Calorific value | Higher heating value, MJ/m3 | 12.7 | 39.8 | 1/3 of natural gas by volume | 3× gas velocity needed to deliver the same amount of |
|  |  |  |  |  | heat energy |
|  |  |  |  |  | 3× energy needed to compress gas |
|  |  |  |  |  | 3× volumetric gas flow measurements needed |
|  |  |  |  |  | 3× less line pack storage |

MARTIN ET AL.

3998  |

## |	Chemical

There are four key chemical differences between H2 and CH4 that relate to their reactivity, flammability, flame properties, and energy density. First, H2 is far more reactive than CH4. CH4 is the least reactive of the hy- drocarbons, and whereas H2's H‐H bond has about the same bond energy as the C‐H bond in CH4, H2's bond symmetry relative to CH4 allows the formation of partial bonds which lower the activation energy of reactions with other molecules relative to methane.16 This means that H2 can more easily react with some construction materials (e.g., cement) and it can be harder to store H2 underground than CH4.

Second, the ignition properties of H2 relative to CH4 make it more flammable. Hydrogen has a much wider range between lower and upper flammability limits than natural gas (4%–75% for H2 vs. 5.3%–15% for CH4 and 5%–15.6% for natural gas).16,17 H2 leakage is, therefore, more likely to reach a potential source of ignition within the range of ignitable mixture concentrations than sim- ilarly sized leaks of natural gas. H2 also has a consider- ably lower ignition energy than CH4, meaning that it is considerably easier to ignite accidentally via arcs and sparks from electrical devices.17

Third, H2's flame properties make it more dangerous than CH4. H2's laminar flame speed is about eight times that of CH4.18 Flame speed affects flame stability in burners, the risk of flashback, and overpressure, which may be encountered during a deflagration event such as the ignition of gas leaked into a confined space. Flames of pure H2 are also very low in visible light emissions, making flame detection more difficult. Finally, H2's adi- abatic flame temperature is higher than that of CH4. This gives it the potential to generate more nitrogen oxides (NOx) for given combustion conditions.17,19

Fourth, H2 has a very high energy density per unit mass, but per unit volume, its energy density is about one‐third that of a typical pipeline gas. This means that much less energy is transmitted, distributed, and stored in the same volume of H2 versus natural gas.

## |	Atmospheric

CH4 is an infrared‐absorbing GHG, whereas H2 is not. However, both gases react with hydroxyl radicals in the atmosphere, leading to increased concentrations of other GHGs and, therefore, indirectly causing warming. For CH4, the main sink of emissions is atmospheric oxidation with the hydroxyl radical that on average takes about a decade, leading to the formation of the GHGs tropo- spheric ozone, stratospheric water vapor, and carbon

dioxide.20 For H2, ~70% is taken up by microbial com- munities in the soil and the remaining ~30% take about 2 years to be oxidized by the hydroxyl radical, leading to the formation of tropospheric ozone and stratospheric water vapor.21,22 An additional warming effect from H2 emitted to the atmosphere is that less hydroxyl is avail- able to react with CH4, thereby increasing its residence time in the atmosphere. Consequently, current assess- ments of hydrogen's global warming potential suggest that H2 can cause around ~12 times more warming than carbon dioxide (CO2) over a 100‐year period following emissions of equal mass, and ~37 times more warming over a 20‐year period.21 CH4's warming potency (from direct and indirect warming effects) is around ~30 and

~80 times that of CO2 over 100 and 20 years, respectively.4

# |	IMPLICATIONS ACROSS THE NATURAL GAS VALUE CHAIN

The physical and chemical differences between H2 and CH4 are critical to the suitability of using several com- ponents of existing natural gas infrastructure for H2, and contribute to safety, energy supply, climate, and cost risks (see Figure 1). Although there are solutions to mitigate some of these risks, they too are often associated with new risks and challenges.

## |	Production

Natural gas is produced from wells and fed via gathering lines to processing plants, where a gas mixture meeting pipeline specifications is produced. Purification processes vary by gas composition but often include removal in part or in total of gaseous higher‐carbon hydrocarbons, butane, propane, ethane, in addition to sulfur com- pounds, mercury, carbon dioxide, water, and rarely, helium. Sometimes, nitrogen is added to reduce the en- ergy content.

Some natural gas production can be expected in a decarbonized future, for use in producing chemicals like ethylene and propylene. However, given that most gas is burned rather than used as a chemical feedstock,23 most natural gas wells, gathering lines, and processing plant infrastructure would only have very limited use in a decarbonized world as peaking capacity to complement renewable power and storage (see Figure 2). Reuse of some components may be possible, with scraps taken and repurposed. Therefore, new infrastructure would be required to scale up hydrogen production facilities and then transport the hydrogen to the natural gas

MARTIN ET AL.

NATURAL GAS

LONG DISTANCE TRANSPORT	•

OJ

SCI

where science

meet,b11Sness

|	3999

.. ..

t... .

-,,:._-t .:

·I,

-,,:--....

....

HYDROGEN

(H,)

Pipeline Material	Compressors	Valves

2	2

H reacts with steel, H	Materials, seals,	 H can leak from atoms diffuse into metal, engines incompatible	closed valves, cracking accelerated	 with H2	 packings etc.

..

••••	••	•••

LOCAL DISTRIBUTION

.. ..

Liquified Gas

H2 needs l 00 °C colder

temperatures than CH

4

to be in liquid form

•••

Pipeline Material

H2 can permeate faster than

natural gas through plastic and

other "soft" materials

••••

Meters

Can underreport flowrate when H2 present

••

STORAGE

g

EN

Equipment Design Equipment is incompatible with H2

•	••••	•

Safety Management

H2 more easily leaks and ignites, flames

difficult to detect; flame instability more

likely, can worsen air quality

••

SAFETY

Flammability hazards; worsened air quality

ENERGY SUPPLY

Reduced reliability;

service interruption

CLIMATE

Climate-worming

gos emissions

COST

lost product and/or

added expense

UNUSABLE

New equipment needed;

stranded assets

FI GURE 1	Challenges and risks with using existing natural gas system for pure hydrogen service.

MARTIN ET AL.

4000	|

FI GURE 2	Existing natural gas production system suitability for pure hydrogen.

transmission infrastructure. However, although natural gas processing plants are not designed for H2, it is pos- sible that some parts may be salvaged and relocated.

## |	Long‐distance transport

Natural gas from processing plants is often transported long distances via transmission pipelines or transported in its liquified form, when crossing oceans. Transmission pipelines typically operate at considerable pressure (50–150 bar or 5–15 MPa); are constructed from high yield strength grades of carbon/low alloy steel; have ex- terior coatings and electrochemical protection to reduce pipe corrosion; and are often buried (or subsea) for physical protection.24 Interior linings are sometimes used. The pipes are sized for pressure drops on the order of 5 psi per mile (20 kPa/km), with compressor stations at regular intervals to maintain pressure. These compres- sors often use centrifugal‐type or reciprocating‐type machines and are powered by gas turbines or engines fueled by the gas in the pipeline, and in some cases electric motor‐driven.24,25

There are several issues with using the current nat- ural gas transmission system for H2, relating to pipeline material, line capacity, valves, and compressors (see Figure 3).26–29 Hydrogen accelerated fatigue cracking (HAFC) is the primary concern in converting existing natural gas pipelines for H2.30–32 In high‐yield strength steels commonly used in gas transmission pipelines, ex- posure to molecular hydrogen combined with cyclic stress, initiated at manufacturing or welding flaws or corrosion points in the piping system, increases the growth rate of cracks. The process, known as HAFC, occurs because hydrogen atoms diffuse into the steel.33 The cracks may ultimately extend through the wall of the pipe, causing it to leak or burst.34 The hydrogen atoms

can also recombine into molecular hydrogen gas at defects in the steel.35 Low‐yield‐strength steel pipes are not particularly susceptible to fatigue cracking unless both temperature and the partial pressure of hydrogen are quite high.30,36

Recent, extensive testing of typical pipeline materials in Europe demonstrates both acceleration of fatigue cracking and reduction in fracture toughness when hydrogen is used, but the impacts vary widely depending on the material.36 Welds and their heat‐affected zones, as well as manufacturing or fabrication defects in the pipe increase vulnerability by serving as crack initiation sites.37 This issue has been known for decades.

Pipe failure is of concern due to potential asphyxia- tion and fire and explosion.38–40 Because natural gas pipes are usually buried, external inspections are difficult and internal inspections are largely relied upon to verify the integrity of the pipe material. Consequently, there is a considerable risk of premature failure if natural gas pipes are re‐purposed for H2 service. There are, however, sev- eral solutions that have been suggested, but none are without additional challenges.

First, hydrogen could be “blended” with natural gas below a certain threshold so that the partial pressure of hydrogen is limited and HAFC risk is reduced.41 How- ever, this significantly limits the decarbonization poten- tial of using hydrogen, because it is not safe to pursue higher blending rates without undertaking retrofits or complete replacement of pipes. Even with small per- centage admixtures of molecular hydrogen in high pressure natural gas pipes made of high‐yield strength carbon steels it is expected that considerable acceleration of fatigue cracking, by as much as 30‐fold, will occur with fracture resistance of the piping material reduced by as much as 50%.34

Second, it is sometimes possible to install a liner or coating into a natural gas pipe to protect it against

MARTIN ET AL.

|

4001

FI GURE 3	Existing natural gas transmission system suitability for pure hydrogen.

corrosion and erosion, leading some to suggest that liners or coatings may provide a means to protect existing gas pipelines against HAFC associated with H2.33,42,43 How- ever, this can be challenging both technically and logisti- cally. Furthermore, H2 permeates through nonmetallic materials and, over time, even permeates through intact metallic materials.44 Thus, the suite of hydrogen‐ impermeable materials to choose from is extremely lim- ited. Moreover, installing a liner in an existing buried line is very difficult to undertake effectively and would require shutting down the pipe for an extended period of time.

Because permeation is likely inevitable, the space between the liner and the inner diameter of the pipe would need to be vented at numerous points along the pipeline, or else the cracking risk would not be prevented. The resulting H2 leakage/venting also represents a flammability hazard and emits climate‐warming H2 into the atmosphere. Research into suitable options for the interior protection of gas pi- pelines against H2‐induced damage is underway, with recent developments identifying graphene and MXene as promising.43 However, liners are difficult to install, con- trol, and inspect regardless of material.

MARTIN ET AL.

4002	|

Third, cyclic stress amplitude can be reduced and HAFC might be delayed by operating piping systems at constant pressure, but practically it may not be possible, and other cyclic stresses (from vibration, soil movements, thermal expansion, and so on) will continue to pose a risk of fatigue cracking. Repurposing existing gas pipe- lines to carry H2 would also often require de‐rating the design pressure to as little as half to one‐third of the original due to design codes and standards (see Sup- porting Information for details).42 A reduction in design pressure of this magnitude represents a very significant reduction in pipeline energy‐carrying capacity and also diminishes the “line pack” (i.e., the energy stored in the form of gas compressed above its delivery pressure in the gas network; discussed further in Section 3.4).

There are safe materials available for construction of

new, purpose‐built H2 pipelines.30,45 Purpose‐built industrial hydrogen pipelines made from mild steels, lower strength steels or high yield strength steels that were designed and fabricated for use with hydrogen have been operating for decades.45,46 The key is design pres- sure determinations, materials selection, nondestructive examinations, welding methods, and testing all focused on H2 applications. These pipelines are operated differ- ently than natural gas pipelines, operating at low and near constant pressures (less than about 65 bar(g) or

6.5 MPa).

Regardless of potential modifications and replace- ment, an additional transmission challenge for hydrogen is pipeline capacity. With H2's energy density per unit volume at one‐third that of a typical natural gas and the desirability of operating hydrogen pipelines at low pres- sure, the ability to move large amounts of hydrogen using existing pipelines is limited. For example, the amount of energy that can be transmitted by hydrogen compared to natural gas would be one ninth if derating pressure by on third and having one‐third of the calorific value.

Alternatively, the volumetric flowrate could be increased so that a given gas transmission pipeline car- rying hydrogen could deliver the same number of joules per hour of heat energy as existing natural gas pipelines.47–49 However, an increase in volumetric flow- rate depends on compressors being able to overcome frictional losses, which would require a lot of energy.47–49 The mechanical energy to compress one gas relative to another is roughly inversely proportional to its molecular weight, which at constant temperature and pressure is proportional to the volumetric flow at a given compres- sion ratio (see Supporting Information). Given that H2 would need to flow in piping at roughly three times the volumetric flowrate of natural gas to deliver the same amount of energy, hydrogen compressors would require at least three times as much energy as those used for

natural gas. Compression energy requirements would be increased further if the design pressure of the piping must also be reduced; a line operating at reduced pres- sure would have reduced energy carrying capacity, and the pressure loss per unit length would require com- pression to a greater compression ratio at each com- pressor station. This would require proportionately more compressor input energy per delivered joule of heat en- ergy in the transmitted gas, thus, undercutting the net climate benefits of delivered hydrogen. (See calculations in Supporting Information.)

Although the energy efficiency impact and cost may be significant, the need to replace all compressors in existing transmission systems with larger machines of considera- bly higher power and suction displacement would require a significant investment and the capacity to provide such compressors. Existing compressors are often made of materials of construction (high strength steels, and so on) and can have seals, and so on, incompatible with H2, and any engines previously running on gas would need replacement or significant modification to operate with pure H2.50 In the absence of valve replacement hydrogen can leak from existing closed valves, packings, and so on, which leads to safety hazards, lost product, and climate‐ warming emissions.50,51

## |	Local distribution

Once delivered to the “city gate,” natural gas is distrib- uted to individual users via an extensive network of buried piping operating at medium to low pressures. These pipelines are made of a variety of materials rang- ing from mild steel to cast iron to high‐density poly- ethylene (HDPE).

The lower pressure in the distribution network, the operation of piping farther away from their yield strength, and the infrequent use of high‐yield strength steels in construction reduces the risk of HAFC. The major con- cerns in the gas distribution network for re‐use with H2 are not primarily associated with metallurgy, but rather with leakage and permeation and associated climate warming and fire/explosion risk (see Figure 4).26,28,29,52

Hydrogen permeates through intact HDPE and other “soft goods” (polymeric and elastomeric materials used in gaskets, seals, and so on) at an appreciable rate.53 The H2 molecule's considerably smaller molecular diameter and high diffusivity relative to CH4 lead to faster per- meation, that is, more molecules of H2 will permeate per unit time than molecules of CH4 at a given pressure. There is also an overall tendency for H2 to leak to a greater extent than that of natural gas.53 Theory suggests that H2 will leak at 1.3–3 times the rate of CH4.54

MARTIN ET AL.

|

4003

FI GURE 4	Existing natural gas distribution system suitability for pure hydrogen.

Measurements confirm the increased H2 leakage rate through plastic piping of four to five times that of natural gas.24,55 However, there are some limited lab experiments that indicate that hydrogen may leak at the same rate56 or faster than methane57 depending on flow regimes.

There is also some evidence of material property changes in HDPE piping after exposure to hydrogen, and additional research is warranted to understand a safe lifetime for HDPE pipes used in the distribution of hydrogen. There doesn't appear to be any safety concern related to premature failure arising from hydrogen ex- posure.55 However, elastomeric materials exposed to hydrogen show reduction in tensile strength due to per- meation, increasing the risk of larger leaks.24

The use of liners to reduce permeability may provide a partial solution, but more research is required.42 Alternatively, blending hydrogen into the gas network for transport is another option to mitigate issues of transporting hydrogen, although it provides limited decarbonization potential. Some have raised the potential of de‐blending when pure H2 is required. Methods including pressure‐ or temperature‐swing adsorption and selective membranes have been examined in detail.24,55 The result would be a significant additional cost and energy demand per kilogram of pure hydrogen re- covered.24 Methane and hydrogen emissions associated with the separation process would also be of concern.

Gas meters in the distribution network would likely need significant retrofit or replacement.26,58 Not only might they be required to measure gas volumetric flows three times as high as those required for fossil gas (to deliver same energy content to consumers), but

diaphragm‐type meters using large elastomeric or poly- meric components have been known to under‐report flowrate when fed gas mixtures containing hydrogen.59

## |	Storage

Natural gas systems contain both large storage elements for management of seasonal variation in gas use and smaller storage elements that manage daily variations in flow. The storage afforded by virtue of the volume of gas held up in the transmission and gas distribution network itself is referred to as “line pack.” Line pack storage, in the form of the difference in pressure between nominal and minimum operating pressure for the gas system in question, can represent many hours of system demand. Such storage, absent from electrical distribution systems, is a critical tool for maintaining gas grid operational stability against fluctuations in demand and supply and against interruptions in service due to equipment failures or maintenance.60

Switching the gas system to pure H2, with an energy density per unit volume roughly one‐third that of a typ- ical pipeline gas; therefore, would result in a reduction in “line pack” storage to one‐third of the present value if storage pressure and volume are kept constant (Figure 5).49 If pipeline design pressures must be de‐rated to accommodate the added risks associated with hydro- gen to the pipeline materials of construction (as dis- cussed in Section 3.2), a further reduction in the line pack would be expected. This would either represent a reduction in reliability and peak flow handling capacity,

MARTIN ET AL.

4004	|

FI GURE 5	Existing natural gas storage system suitability for pure hydrogen.

or a need to install new dedicated storage not currently required on the network.

In most heating climates where gas use is much higher in winter than summer, additional gas storage is often incorporated into the gas network to provide a seasonal buffer. The volumes of gas involved are large, such that the use of above‐ground storage facilities (such as the gas‐o‐meters previously used in the age of town gas) has largely been rendered impractical. Subsurface gas storage in depleted gas reservoirs, constructed salt caverns, and aquifers will be required to balance the system if there is variation in demand, yet H2 is both geologically and biologically reactive.61 Storing H2 in depleted reservoirs formerly containing natural gas is possible but will likely result in depleted product.55,62,63 Furthermore, uses such as fuel cells that require high purity hydrogen may be impaired if hydrogen has been contaminated due to storage in a former gas reservoir.64 On the other hand, using salt caverns for hydrogen storage should not compromise the integrity of hydrogen as it should not react with salt, and salt caverns are used today for natural gas storage.65,66 However, suitable geology may not be available where storage capacity is required and not all salt domes are pure salt. Given the difficulties associated with using depleted natural gas reservoirs to store hydro- gen, construction of “salt dome” storage facilities could

represent a significant additional cost.14

## |	End use

Equipment (appliances, devices, and so on) designed to burn or derive energy from a gas mixture is optimized around the properties of that gas mixture. The tolerance for variations in gas properties, notably energy density per unit volume, flame speed, adiabatic flame tempera- ture, explosive range, and the Wobbe index (an indicator of the interchangeability of fuel gases in combustion equipment) varies with the type of device. Most natural gas end‐user devices can tolerate hydrogen additions to natural gas mixtures of up to about 20% by volume (about 7% in terms of energy content) without requiring signif- icant modification.24,55,67–71

However, very few appliances or end‐user devices designed to use fossil gas mixtures are suitable for use with pure H2 without significant modification or replacement.72 Natural gas devices and appliances are incompatible with pure H2 because of the physical and chemical dif- ferences between CH4 and H2 (Table 1). Hydrogen's smaller size allows it to escape more easily and permeate through materials, risking explosive‐level concentrations and climate‐warming emissions.15 Hydrogen's lower den- sity also causes it to rise and accumulate at high points in enclosed spaces. Although the difference in buoyancy is somewhat offset by hydrogen's greater diffusivity, the

greater diffusivity can lead to more rapid leakage.

MARTIN ET AL.

|

4005

H2 is also more explosive, ignitable, burns hotter, and the flame is faster with lower visibility than CH4; these characteristics yield higher safety risks. The significant differences in properties between typical natural gas mix- tures and H2, therefore, necessitate changes in the design of burners and burner management systems to achieve com- parative levels of safety, which must then be certified (Figure 6).17,67 For example, all H2 burner appliances require flame failure detection apparatus such as that used in the burners for ovens and broilers that shuts off the flow of gas when ignition does not result in a rise in gas tem- perature within a few seconds of the gas valve opening.

A quantitative risk assessment (QRA) was carried out in advance of a planned trial of pure H2 in a residential gas distribution system in the UK.18 The report con- cluded that even if the homes were fitted with appliances designed and certified for use with H2, the risk of damage and injury due to fires and explosions would increase in frequency and severity. The report recommended that in addition to a leak testing program, excess flow devices of dissimilar type be installed in every home operating with H2 (something, i.e., not currently done for natural gas supplies). One such device would be a conventional ex- cess flow valve, which closes when flow through the valve greatly exceeds the maximum expected flow (due to, for instance, damage to a downstream pipe). Another would be a “smart meter,” with an automated valve in- terlocked to close when the gas meter reported gas flow greater than the expected maximum. However, these devices were only expected to reduce the severity of fires and explosions, but not the frequency—therefore, the QRA asserted that injuries and deaths would be approximately the same as those encountered with ex- isting gas use, even though events would be more fre- quent fires and explosions. The report also recommended that each room containing a gas appliance be fitted with a 10 × 10 cm nonclosing vent within 1.5 m of the ceiling, connected to the outdoors, to serve to vent any H2 accumulating during a leakage event. Such vents would create a significant loss of heat and decreased comfort due to drafts, and therefore increased heating fuel use for the residents.

An additional safety challenge is the use of stenching agents, which are added to gas in the low‐pressure distribution system to aid in leakage detection. Conven- tional sulfur‐containing stenching agents, such as mer- captan used in the natural gas systems, are powerful fuel cell catalyst poisons.64 However, they can be used as long as fuel cells are not deployed or are fitted with adsorbents to remove the stenching agent at the point of use, but this risks fuel cell failure.73 Some previous research that has tested promising odorants compatible with fuel cells, but none appear commercially available. 74,75

Finally, although H2 combustion would eliminate the toxic risk of carbon monoxide—a consequence of natural gas combustion—it would not eliminate NOx emissions that all fuels generate when burned in air, by virtue of the reaction of atmospheric nitrogen with oxygen. The hotter hydrogen flame could yield more NOx emissions than natural gas.71,72,76,77 Hydrogen combustion pro- duces NO, which rapidly oxidizes to form NO2, a pollu- tant regulated globally. NO2 is a major health risk and is linked to childhood asthma among other ailments.78 Residential and small commercial/industrial combustion equipment either vent into the room air (cooktops/hobs/ ovens) or via a flue to the outdoors (boilers, furnaces), but without catalytic NOx reduction equipment.79–81 For devices with an enclosed flue (furnaces, boilers, and so on), catalytic NOx reduction is possible but is expensive and high‐maintenance, because a reducing agent is required which must be replenished.

# |	DISCUSSION AND CONCLUSION

Replacing natural gas with zero‐ and low‐carbon hydro- gen is viewed by many as an attractive decarbonization tool, because it can potentially re‐use expensive infra- structure of considerable economic value. However, this paper has shown that there are numerous unresolved challenges with using hydrogen in the existing natural gas infrastructure due to its differing physical and chemical qualities compared to methane, the main component of natural gas. These differences have major implications for the entire natural gas value chain— encompassing production, long‐distance transport, local distribution, storage, to end use. The existing infra- structure is mostly unusable without de‐rating to lower pressures (with consequently much decreased energy flow rates) or substantial investments, which often rely on unproven solutions. In addition, end‐use appliances need replacement, and even then, they would still have safety and health challenges that would need to be overcome with new solutions.

Although many of the concerns associated with deploying pure hydrogen energy systems can be mitigated by blending hydrogen with natural gas, doing so will not help decarbonize the economy as it does not facilitate a gradual transition to pure hydrogen, and it only offers a small reduction in GHG emissions. The benefits from reduced GHG emissions are limited due to the greatly lower volumetric energy density of hydrogen relative to the gas it displaces. For example, a mixture of 20% hydrogen (by volume) into natural gas is only about 7% hydrogen in terms of energy content and, in the best case,

MARTIN ET AL.

4006	|

FI GURE 6	Existing natural gas end use system suitability for pure hydrogen.

represents only a 7% reduction in carbon dioxide emis- sions per joule of heat generated by its combustion. Fur- thermore, blending hydrogen with natural gas still has safety and climate risks from leakage and NOx emissions. Overall, while repurposing the natural gas system for use with hydrogen may, at first, seem appealing, the limited practicality, risks, and data gaps strongly suggest that like‐for‐like gas substitution provides limited

benefits for increased risks, even if major technical and economic hurdles are overcome.

That said, continuing to rely on natural gas is also not a viable option for addressing the climate crisis. Considering its physical and chemical properties, hydrogen is not an effective decarbonization tool for use in homes and build- ings. For any decarbonization strategy, it is critical to deter- mine if a fuel is in fact needed, and to compare with

MARTIN ET AL.

|

4007

potentially more effective options such as direct electrifica- tion using renewably generated electricity.

ACKNOWLEDGMENTS

The authors thank Stephane Sartzetakis and Dr. Shradda Dhungel for their support in preparing the manuscript. Any opinions and conclusions expressed herein are those of the authors and do not necessarily reflect the views or policies of the U.S. Government. This work was primarily completed while Dr. Ocko was at Environmental Defense Fund.

ORCID

Ilissa B. Ocko  https://orcid.org/0000-0001-8617-2249 Sofia Esquivel‐Elizondo  https://orcid.org/0000-0001- 8946-9654

REFERENCES

- IEA. Greenhouse Gas Emissions from Energy Data Ex- plorer, 2023.

- Global Carbon Project. Supplemental Data of Global Carbon Budget (Version 1.0) [Data set], 2022.

- IEA. Global Methane Tracker, 2023. https://www.iea.org/ reports/global-methane-tracker-2023

- IPCC. Summary for policymakers. In: Masson‐Delmotte V, ed. Climate Change 2021 – The Physical Science Basis. Cambridge University Press. 3‐32. 2023. https//doi.org/10.1017/

9781009157896.001

- UNFCCC. Conference of the Parties (COP28) to the UN Framework Convention on Climate Change (UNFCCC). COP28: The UAE Consensus, Dubai, 2023.

- Smolinka T, Bergmann H, Garche J, Kusnezoff M. Chapter 4 ‐ The history of water electrolysis from its beginnings to the present. In: Smolinka T, Garche J, eds., Electrochemical Power Sources: Fun- damentals, Systems, and Applications. Elsevier; 2022:83‐164.

- Prinzhofer A, Cissé CST, Diallo AB. Discovery of a large accumulation of natural hydrogen in Bourakebougou (Mali). Int J Hydrogen Energy. 2018;43:19315‐19326.

- Hydrogen Council. Hydrogen Insights 2023: An Update on the State of the Global Hydrogen Economy, with a Deep Dive into North America, 2023. https://hydrogencouncil.com/en/ hydrogen-insights-2023/

- Bauer C, Treyer K, Antonini C, et al. On the climate impacts of blue hydrogen production. Sustain Energy Fuels. 2022;6:66‐75.

- Ocko IB, Hamburg SP. Climate consequences of hydrogen emissions. Atmos Chem Phys. 2022;22:9349‐9368.

- de Kleijne K, de Coninck H, van Zelm R, Huijbregts MAJ, Hanssen SV. The many greenhouse gas footprints of green hydrogen. Sustain Energy Fuels. 2022;6:4383‐4387.

- Giovanniello MA, Cybulsky AN, Schittekatte T, Mallapragada DS. The influence of additionality and time‐matching requirements on the emissions from grid‐connected hydrogen production. Nat Energy. 2024;9:197‐207. doi:10.1038/s41560-023-01435-0

- Sun T, Shrestha E, Hamburg SP, Kupers R, Ocko IB. Climate impacts of hydrogen and methane emissions can considerably reduce the climate benefits across key hydrogen use cases and time scales. Environ Sci Technol. 2024;58:5299‐5309. doi:10. 1021/acs.est.3c09030

- Sadler D. Leeds City Gate (Report: H21). City of Leeds; 2016. https://www.northerngasnetworks.co.uk/wp-content/ uploads/2017/04/H21-Report-Interactive-PDF-July-2016. compressed.pdf

- Scholand M. Debunking the Hydrogen Hype: Why Europe Should Pursue Electrification Instead of Hydrogen for Cooking and Heating. Environmental Coalition on Standards (ECOS); 2024. https://ecostandard.org/wp-content/uploads/2024/05/Debunking- the-Hydrogen-Hype_M2S2-Energy-Ltd2.pdf

- Crabtree RH. Aspects of methane chemistry. Chem Rev. 1995;95:987‐1007.

- Klebanoff LE, Pratt JW, LaFleur CB. Comparison of the safety‐ related physical and combustion properties of liquid hydrogen and liquid natural gas in the context of the SF‐BREEZE high‐ speed fuel‐cell ferry. Int J Hydrogen Energy. 2017;42:757‐774.

- Brown S, Posta G, McLaughlin P. Work Package 7 Safety Assessment: Conclusions Report (Incorporating Quantitative Risk Assessment. ARUP and Kiwa Gastec; 2021. https://static1. squarespace.com/static/5b8eae345cfd799896a803f4/t/ 60e399b094b0d322fb0dadc4/1625528759977/conclusions+inc

+QRA.pdf

- United States Environmental Protection Agency (EPA). Nitrogen Oxides (NOx), Why and How They Are Controlled. http://www.epa.gov/ttn/catc (1999).

- Szopa S, Naik V. Short‐lived climate forcers. In: Masson‐ Delmotte V, eds. Climate Change 2021: The Physical Science Basis. Contribution of Working Group I to the Sixth Assessment Report of the Intergovernmental Panel on Climate Change. Cambridge University Press; 2021:817‐922.

- Sand M, Skeie RB, Sandstad M, et al. A multi‐model assess-

ment of the Global Warming Potential of hydrogen. Commun Earth Environ. 2023;4:203.

- Warwick NJ, Archibald AT, Griffiths PT, et al. Atmospheric composition and climate impacts of a future hydrogen econ- omy. Atmos Chem Phys. 2023;23:13451‐13467.

- U.S. Energy Information Administration (eia). Natural gas expected to remain most‐consumed fuel in the U.S. industrial sector. Today in Energy, 2018.

- Melaina MW, Antonia O, Penev M. Blending Hydrogen into Natural Gas Pipeline Networks: A Review of Key Issues. National Renewable Energy Laboratory; 2013. doi:10.2172/1068610

- Interstate Natural Gas Association of America (INGAA).

Interstate Natural Gas Pipeline Efficiency. Vol 32, 2010.

- Erdener BC, Sergi B, Guerra OJ, et al. A review of technical and regulatory limits for hydrogen blending in natural gas pipelines. Int J Hydrogen Energy. 2023;48:5595‐5617.

- San Marchi C, Somerday BP, Nibur KA. Development of methods for evaluating hydrogen compatibility and suitability. Int J Hydrogen Energy. 2014;39:20434‐20439.

- Gislon P, Cerone N, Cigolotti V, et al. Hydrogen blending effect on fiscal and metrological instrumentation: a review. Int J Hydrogen Energy. 2024;67:1295‐1307. doi:10.1016/j.ijhydene.2024.02.227

- Tian X, Pei J. Study progress on the pipeline transport- ation safety of hydrogen‐blended natural gas. Heliyon. 2023;9:e21454.

- Jones D. Principles and Prevention of Corrosion. Prentice Hall; 1992.

- Kappes MA, Perez T. Hydrogen blending in existing natural gas transmission pipelines: a review of hydrogen embrittlement,

MARTIN ET AL.

4008	|

governing codes, and life prediction methods. Corrosion Rev. 2023;41:319‐347.

- Wu X, Zhang H, Yang M, Jia W, Qiu Y, Lan L. From the perspective of new technology of blending hydrogen into natural gas pipelines transmission: Mechanism, experimental study, and suggestions for further work of hydrogen embrit- tlement in high‐strength pipeline steels. Int J Hydrogen Energy. 2022;47:8071‐8090.

- Zhu YQ, Song W, Wang HB, et al. Advances in reducing hydrogen effect of pipeline steels on hydrogen‐blended natural gas transportation: a systematic review of mitigation strate- gies. Renew Sustain Energy Rev. 2024;189:113950. doi:10. 1016/j.rser.2023.113950

- Ronevich J, Somerday B. Assessing gaseous hydrogen assisted fatigue crack growth susceptibility of pipeline steel weld fusion zones and heat affected zones. Mater Perform Charact. 2016;5:290‐304.

- Nykyforchyn H, Unigovskyi L, Zvirko O, Tsyrulnyk O, Krechkovska H. Pipeline durability and integrity issues at hydrogen transport via natural gas distribution network. Proc Struct Integrity. 2021;33:646‐651.

- Steiner M, Marewski U, Silcher H. DVGW Project SyWeSt H2: Investigation of Steel Materials for Gas Pipelines and Plants for Assessment of Their Suitability with Hydrogen. DVGW Research Project Group; 2023.

- Jia G, Lei M, Li M, et al. Hydrogen embrittlement in hydrogen‐blended natural gas transportation systems: a review. Int J Hydrogen Energy. 2023;48:32137‐32157.

- Rusin A, Stolecka K. Modelling the effects of failure of pipe- lines transporting hydrogen. Chem Process Eng. 2011;32(No 2 June):117‐134.

- Rusin A, Stolecka K. Hazards associated with hydrogen infrastructure. J Power Technol. 2017;97:153‐157.

- Witkowski A, Rusin A, Majkut M, Stolecka K. Comprehensive analysis of hydrogen compression and pipeline transportation from thermodynamics and safety aspects. Energy. 2017;141: 2508‐2518.

- Lipiäinen S, Lipiäinen K, Ahola A, Vakkilainen E. Use of existing gas infrastructure in European hydrogen economy. Int J Hydrogen Energy. 2023;48:31317‐31329.

- Khan TO, Young MA, Layzell CB. The Techno‐Economics of Hydrogen Pipelines. Transition Accelerator Technical Briefs. Vol 1. The Transition Accelerator; 2021:1‐40. https:// transitionaccelerator.ca

- Cristello JB, Yang JM, Hugo R, Lee Y, Park SS. Feasibility analysis of blending hydrogen into natural gas networks. Int J Hydrogen Energy. 2023;48:17605‐17629.

- Emerson. Rosemount pressure transmitters. For more infor- mation on Rosemount pressure transmitters: Material selec- tion and compatibility considerations for rosemount. Pressure Transmitters, 2018.

- Mohitpour Mo, Solanky H, Vinjamuri GK. Materials selection and performance criteria for hydrogen pipeline transmission. Flaw Evaluation, Service Experience, and Materials for Hydro- gen Service. ASMEDC; 2004:241‐251. doi:10.1115/ PVP2004-2564

- U.S. Department of Energy Pipeline Working Group Work- shop. Hydrogen Pipeline Working Group Workshop Proceed- ings. U.S. Department of Energy, Energy Efficiency &

Renewable Energy: Hydrogen, Fuel Cells, and Infrastructure Technologies Program; 2005.

- Abbas AJ, Hassani H, Burby M, John IJ. An investigation into the volumetric flow rate requirement of hydrogen transpor- tation in existing natural gas pipelines and its safety implica- tions. Gases. 2021;1:156‐179.

- Cristello JB, Yang JM, Hugo R, Lee Y, Park SS. Feasibility analysis of blending hydrogen into natural gas networks. Int J Hydrogen Energy. 2023;48:17605‐17629.

- Klopčič N, Stöhr T, Grimmer I, Sartory M, Trattner A. Refur- bishment of natural gas pipelines towards 100% hydrogen—a thermodynamic‐based analysis. Energies. 2022;15:9370.

- Kurz R, Winkelmann B, Freund S, et al. Chapter 6 ‐ Transport and storage. In: Brun K, Allison T, eds. Machinery and Energy Systems for the Hydrogen Economy. Elsevier; 2022:215‐249. doi:10.1016/B978-0-323-90394-3.00003-5

- Riemer M, Schreiner F. Conversion of LNG Terminals for Liquid Hydrogen or Ammonia Analysis of Technical Feasibility under Economic Considerations Conversion of LNG Terminals for Liquid Hydrogen or Ammonia Project Coordination Responsible for Content. Fraunhofer; 2022.

- Zhou C, Yang Z, Chen G, Zhang Q, Yang Y. Study on leakage and explosion consequence for hydrogen blended natural gas in urban distribution networks. Int J Hydrogen Energy. 2022;47:27096‐27115.

- Morgan G. Understanding hydrogen permeation testing on non‐ metallic materials. Element; 2023.

- Swain M, Swain M. A comparison of H2, CH4 and C3H8 fuel leakage in residential settings. Int J Hydrogen Energy. 1992;17: 807‐815.

- Topolski K, Reznicek EP, Erdener BC, et al. Hydrogen Blending into Natural Gas Pipeline Infrastructure: Review of the State of Technology. NREL; 2022. https://www.nrel.gov/ publications

- Hormaza Mejia A, Brouwer J, Mac Kinnon M. Hydrogen leaks at the same rate as natural gas in typical low‐pressure gas infrastructure. Int J Hydrogen Energy. 2020;45:8810‐8826.

- Penchev M, Lim T, Todd M, et al. Hydrogen Blending Impacts Study Final Report. Agreement Number: 19NS1662, 2022. https://docs.cpuc.ca.gov/PublishedDocs/Efile/G000/M493/ K760/493760600.PDF

- Lo Basso G, Pastore LM, Sgaramella A, Mojtahed A, de Santoli L. Recent progresses in H2NG blends use down- stream Power‐to‐Gas policies application: an overview over the last decade. Int J Hydrogen Energy. 2024;51:424‐453.

- Jaworski J, Kułaga P, Blacharski T. Study of the effect of addition of hydrogen to natural gas on diaphragm gas meters. Energies. 2020;13:3006.

- Cembalest M. Electravision: 14th Annual Eye on the Market Energy Paper. JP Morgan; 2024.

- Zivar D, Kumar S, Foroozesh J. Underground hydrogen stor- age: a comprehensive review. Int J Hydrogen Energy. 2021;46: 23436‐23462.

- Hanson AG, Kutchko B, Lackey G, et al. Subsurface Hydrogen and Natural Gas Storage (State of Knowledge and Research Recommendations Report), 2022. doi:10.2172/1846632

- Muhammed NS, Haq MB, Al Shehri DA, et al. Hydrogen storage in depleted gas reservoirs: a comprehensive review. Fuel. 2023;337:127032.

MARTIN ET AL.

|

4009

- Ohi JM, Vanderborgh N, Gerald Voecks Consultants. Hydro- gen Fuel Quality Specifications for Polymer Electrolyte Fuel Cells in Road Vehicles. U.S. Department of Energy; 2016.

- Ozarslan A. Large‐scale hydrogen energy storage in salt cav- erns. Int J Hydrogen Energy. 2012;37:14265‐14277.

- Linde. Storing Hydrogen in Underground Salt Caverns: Hydrogen Storage, 2021.

- Schiro F, Stoppato A, Benato A. Modelling and analyzing the impact of hydrogen enriched natural gas on domestic gas boilers in a decarbonization perspective. Carbon Resour Convers. 2020;3:122‐129.

- Sun M, Huang X, Hu Y, Lyu S. Effects on the performance of domestic gas appliances operated on natural gas mixed with hydrogen. Energy. 2022;244:122557.

- Guandalini G, Colbertaldo P, Campanari S. Dynamic model-

ing of natural gas quality within transport pipelines in pres- ence of hydrogen injections. Appl Energy. 2017;185:1712‐1723.

- Guzzo G, Cheli L, Carcasci C. Hydrogen blending in the Italian scenario: Effects on a real distribution network con- sidering natural gas origin. J Clean Prod. 2022;379:134682.

- Gondal IA. Hydrogen integration in power‐to‐gas networks.

Int J Hydrogen Energy. 2019;44:1803‐1815.

- Leicher J, Schaffert J, Cigarida H, et al. The impact of hydrogen admixture into natural gas on residential and commercial gas appliances. Energies. 2022;15:777.

- Kopasz J. Fuel cells and odorants for hydrogen. Int J Hydrogen Energy. 2007;32:2527‐2531.

- Mouli‐Castillo J, Bartlett S, Murugan A, et al. Olfactory appraisal of odorants for 100% hydrogen networks. Int J Hydrogen Energy. 2020;45:11875‐11884.

- Imamura D, Akai M, Watanabe S. Exploration of hydrogen odorants for fuel cell vehicles. J Power Sources. 2005;152:226‐232.

- Choudhury S, McDonell VG, Samuelsen S. Combustion per- formance of low‐NOx and conventional storage water heaters operated on hydrogen enriched natural gas. Int J Hydrogen Energy. 2020;45:2405‐2417.

- Wright ML, Lewis AC. Emissions of NOx from blending of hydrogen and natural gas in space heating boilers. Element Sci Anthrop. 2022;10:00114.

- Gruenwald T, Seals BA, Knibbs LD, Hosgood HD. Population attributable fraction of gas stoves and childhood asthma in the United States. Int J Environ Res Public Health. 2022;20:75.

- Lewis AC. Optimising air quality co‐benefits in a hydrogen economy: a case for hydrogen‐specific standards for NOx emissions. Environ Sci Atmos. 2021;1:201‐207.

- Hu Y, Zhao B. Relationship between indoor and outdoor NO2: a review. Build Environ. 2020;180:106909.

- Delabroy O, Haile E, Lacas F, et al. Passive and active control of NOx in industrial burners. Exp Therm Fluid Sci. 1998;16: 64‐75.

SUPPORTING INFORMATION

Additional supporting information can be found online in the Supporting Information section at the end of this article.

How to cite this article: Martin P, Ocko IB, Esquivel‐Elizondo S, et al. A review of challenges with using the natural gas system for hydrogen. Energy Sci Eng. 2024;12:3995‐4009. doi:10.1002/ese3.1861